|  | # FACULTY OF FOUNDRY ENGINEERING ## INTERNATIONAL WORKSHOP 90 Years of Educating Foundry Engineers by the AGH University of Science and Technology in Krakow ## connected with ## XXXVI SCIENTIFIC CONFERENCE FOUNDRYMAN' DAY 2012 ## Krakow, 22 – 23 Nov. 2012 |  |
| --- | --- | --- |

STRENGTH PARAMETERS AND A MECHANICAL RECLAMATION TOGETHER WITH THE MANAGEMENT OF ITS BY-PRODUCTS

J. Kamińska1, A. Kmita1, J. Kolczyk1 and P. Malatyńska1

1 AGH University of Science and Technology. Faculty of Foundry Engineering. 
Reymonta 23, 30-059 Krakow, Poland

1kaminska@agh.edu.pl; 1akmita@agh.edu.pl; 1kolczyk@agh.edu.pl; 1paulina_malatynska@o2.pl

Keywords: Furan resin, Moulding sands, Reclaimed, After reclamation dust, Granulation

Abstract

Selfsetting sands with furan resins are still the largest use of SMS with synthetic resins. They can be used to prepare such forms and cores - of different sizes and shapes, for casting all type alloys [1-3].

A reclamation of spent moulding sands, as a recycling method of waste foundry materials, originated from the casting production cycle, constitutes a very serious problem of each foundry plant, related first of all to the environment protection and also to the rational material management.

The results of furan resin sands strength tests from the matrix of pure quartz sand reclaimed was performed on the test apparatus AT-2. Sand sieve analysis was made of fresh and reclaimed material, and loss on ignition tests conducted on reclaimed material, obtained at different times of reclamation treedment.

Granulation tests of post out reclamation dust, obtained from the sand were also carried 
of furan resin.

Investigations were divided into the following stages:

1 stage: Preparation of the moulding sand with furan resin with sand grains of fresh high-silica sand of the following composition:

| high-silica sand - | 100 parts by mass, |
| --- | --- |
| furan resin U404 - | in various amounts (0.8; 1.0; 1.2 parts by mass), |
| hardener 100T3 - | in various amounts (0.3; 0.5; 0.7 parts by mass). |

2 stage:  Making shaped samples for testing the bending strength Rgu and tensile strength Rmu.

3 stage: Performing the secondary reclamation of the moulding sand in the testing apparatus AT-2, at the impact-abrasive element rotational speed being 460 rot/min. The reclamation time was successively: 5, 10, 15 and 20 minutes.

4 stage: Blowing away the reclaim in the cascade classifier in order to remove dust fractions from the reclaimed material, air velocity: 1 m/s, time: 4 minutes.

5 stage: Preliminary granulation tests of after reclamation dusts originated from the moulding sand with furan resin – in the experimental device.

Fig. 1. Comparison of bending strength of SMS, containing 1.0 part. mas. weight furan resin with different amount of hardener

Acknowledgements

The study was performed within the ‘Dean’s Grant’ 2012  No.15.11.170.417.

References

- Praca zbiorowa pod redakcją: J. Dańko, M. Holtzer: Możliwości ograniczenia i metody zagospodarowania odpadów z procesów odlewniczych. Wydawnictwo Naukowe AKAPIT, Kraków (2009).

- Lewandowski J.L.: Tworzywa na formy odlewnicze. Wydawnictwo „Akapit”, Kraków, 1997.

- Dańko J. Dańko R. Łucarz M.: Procesy i urządzenia do regeneracji osnowy zużytych mas formierskich. Wydawnictwo „Akapit”, Kraków 2007

- Holtzer M., Drożyński D., Bobrowski A., Mazur M., Isendorf B.: Ocena wpływu regeneratu na właściwości mas z żywicą furanową. Archives of Foundry Engineering, Vol. 10, Special Issue 2/2010, 61 – 64.

- Dańko R.: Innovative developments in sand reclamation technologies. Metalurgija – Metallurgy 50(2), 2011, 93-96.

- Dańko R., Holtzer M.: Moulding sands grain size investigations by means of the laser method of measurement. Archives of Metallurgy and Materials 55(3), 2010, 787-794.

- Dańko R., Holtzer M., Danko J.: Reclamation of alkaline spent moulding sands 
of organic and inorganic type and their mixtures. Archives of Foundry Engineering 11(4),  2011, 25-30.

- Dańko R.: Analysis of effectiveness of used sands reclamation treatment – in various technological devices. Archives of Foundry Engineering 9(4), 2009, 31-36.

- Kamińska J., Skrzyńki M.: Physical, chemical and strength properties of dust from the bentonite sands treatment plants. Metallurgy and Foundry Engineering 37(2), 2010, 
189-195.