|  | # FACULTY OF FOUNDRY ENGINEERING ## INTERNATIONAL WORKSHOP 90 Years of Educating Foundry Engineers by the AGH University of Science and Technology in Krakow ## connected with ## XXXVI SCIENTIFIC CONFERENCE FOUNDRYMAN' DAY 2012 ## Krakow, 22 – 23 Nov. 2012 |  |
| --- | --- | --- |

THE CORROSION RESISTANCE OF STAINLESS STEELS AFTER MW PLASMA TREATMENT

D. Kasprzyk1,  B. Stypuła2

AGH University of Science and Technology. Faculty of Foundry Engineering. Reymonta 23, 30-059 Krakow, Poland

1kasprzyk1983@gmail.pl; 2stypula@agh.edu.pl;

Keywords: plasma treatment, corrosion, stainless steels

Abstract

The austenitic stainless steels S32404 and S32615 (chemical composition Tab.1) were subject to the  plasma treatment by deposition of SiCxNy(H) layers The treatment ware performed in the electron cyclotron resonance (ECR) micro wave plasma  system - MWCVD, (2,45GHz 800W) with application of CH4, N2, SiH4 and H2 gas mixture introduced to the reactor.

The corrosion resistance of the samples was determined on the basis of LSV polarization curves in 3% sodium chloride solution at 37°C. The shape of the polarization LSV curves, Fig.1 and optical image of surfaces, Fig. 2 – 3, indicate that the deposited layers improve the corrosion resistance of both steels, particularly the pitting corrosion in the presence of chloride ions, at an elevated temperature. However, the higher resistance has been found when the SiCxNy (H)  layer  was deposited on S32615 stainless steel.

Table. 1. Chemical composition of steels

| Gatunek stali | Zawartość [% mas.] |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C | Si | Mn | P | S | Cr | Ni | Mo | N2 |
| S31603 | 0,02 | 0,55 | 1,60 | 0,03 | 0,03 | 16,54 | 10,1 | 2,02 | 0,064 |
| S32615 | 0,07 | 5,5 | 1,9 | - | - | 18,5 | 21,0 | 1,2 | - |

a)							b)

Fig. 1. Polarization curves LSV: a) S31603, b) S32615

a)				b)

Fig. 2. Sufrace of S31603 after polarization: a) raw, b)treated

a)				b)

Fig. 3. Sufrace of S32615 after polarization: a) raw, b)treated

The resistance is related to the chemical composition of steels. It is significantly affected by the alloy additives, especially silicon [1].

Acknowledgements:

The research was realized with support of the Ministry of Science and Higher Education Republic of Poland (project no.  15.11.170. 453)

References

- Kasprzyk D., Stypuła B., Kuśtrowski P., Drozdek M., The role of mw plasma treatment on the corrosion resistance of stainless steels, Archives of Metallurgy and Materials- in press