|  |  |  |
| --- | --- | --- |
| agh_znk_wbr_rgb_150ppi | FACULTY OF FOUNDRY ENGINEERINGINTERNATIONAL WORKSHOP***90 Years of Educating Foundry Engineers by the******AGH University of Science and Technology in Krakow***connected with XXXVI SCIENTIFIC CONFERENCE FOUNDRYMAN' DAY 2012 Krakow, 22 – 23 Nov. 2012 |  |

**THE INFLUENCE OF GLASSEX ADDITIVE ON PROPERTIES OF MICROWAVE-HARDENED AND SELF-HARDENED MOULDING SANDS WITH WATER GLASS**

K. Major-Gabryś1, St.M. Dobosz2, J. Jakubski3, M. Stachowicz4, D. Nowak5

1, 2,3 AGH University of Science and Technology. Reymonta 23, 30-059 Krakow, Poland

4, 5 Foundry and Automation Team, Wroclaw University of Technology,
ul. Łukasiewicza 5, 50-371 Wroclaw, Poland

1katmg@agh.edu.pl

**Keywords**: Moulding sand, Water glass, Ester hardener, Microwave-hardening

**Abstract**

Requirements for high castings quality cause scientific investigations leading to obtain moulding and core sands having not only good technological properties, but also being environmental friendly [1-4]. In the Department of Moulding Materials on Faculty of Foundry Engineering AGH (University of Science and Technology) there were investigations taken to elaborate new binding systems based on ecological inorganic binders. The biggest group are the moulding sands with hydrated sodium silicate called moulding sands with water glass. Unfortunately inorganic binder character causes mouldings’ low knock-out properties and their low ability to mechanical reclamation. Authors’ research on the first stage considered elaborating and patenting moulding sands with new Glassex additive having improved knock-out properties. In the previous publications, authors [5-10] showed that inserting a new additive Glassex to moulding sands with water glass carried out in ester technology improved their knock-out properties defined (measured) according to technological test [5-8] and according to retained strength examination [5, 8-10]. Authors’ research proved that microwave hardening lets lowing the binder content what makes their knock-out properties better [11-13]. In this paper the influence of different hardeners and the technology of hardening on bending strength and knock-out properties measured by retained strength investigation of moulding sand with water glass and the Glassex additive.

The applied in the article research shows:

* microwave-hardened moulding sands have better strength properties then self-hardened moulding sands. The worst bending strength has the self-hardened moulding sand with ixional SD hardener.
* microwave-hardened moulding sand with water glass and Glassex additive has much higher retained strength in the range of temperature 100-500oC than self-hardened moulding sands prepared in ester technology with all used types of ester hardeners. In the range of temperature 700-1100oC the retained strength of microwave-hardened is lower than retained strength of self-hardened moulding sands with different ester hardeners.

**Acknowledgements**

Scientific research financed from AGH, No 11.11.170.318 – 3/12

**References**

1. Jelinek P., Binding systems of foundry moulding sands, Ostrava (2004) (in Czech).
2. Baliński A., Izdebska-Szanda I., Influence of morphoactive agents of the soluble sodium silicate on temperature changes in moulding sands with this binder, Archives of Mechanical Technology and Automation (2004) 19-29 (in Polish).
3. Baliński A., Stechman M., Różycka D., Influence of modification of the soluble sodium silicate with morphoactive agents on the mechanical properties of the moulding sands in temperatures to 900oC, Materials Engineering, vol.10, no.3 (2003) 271-274.
4. Herecova L., Jelinek P., Esters of carbon acid – hardeners for binders based on sodium silicate, Transactions of the VŚB – Technical University of Ostrava (2006) 79-86 (in Czech).
5. Dobosz St. M., Major-Gabryś K., The new additive to the moulding sands with water glass, DOKSEM 2003, Słowacja, Rajecke Teplice (2003) 38 – 41 (in Polish).
6. Dobosz St. M., Major-Gabryś K., The new way of upgrading the moulding sand’s with water Glass knock-out properties, Materials of the XXVII Scientific Conference for Foundryman Day 2003, Krakow (2003) 81-85 (in Polish).
7. Dobosz St.M., Major-Gabryś K., The surface phenomena in contest of moulding sands’ with water Glass knock-out properties, Archives of Mechanical Technology and Automation (2004) 49-56 (in Polish).
8. Dobosz St.M., Major-Gabryś K., Glassex – The new additive upgrading moulding sand’s with water Glass knock-out properties, Archives of Foundry Engineering, vol. 4, No 13 (2004) 63-68 (in Polish).
9. Major-Gabryś K., Dobosz St.M., The estimation of knock-out properties of moulding sands with water glass and Glassex additive, Materials of the XXVIII Scientific Conference for Foundryman Day 2004, Krakow (2004) 83-87 (in Polish).
10. Dobosz St.M., Jelinek P., Major-Gabryś K, Development tendencies of moulding and core sands, China Foundry, vol. 8, No 4 (2011) 438-446.
11. Stachowicz M., Granat K., Nowak D., Influence of water-glass grade and quantity on residual strength of microwave-hardened moulding sands. Part 1, Archives of Foundry Engineering, vol. 11, No 1 (2011) 93-98.
12. Stachowicz M., Granat K., Nowak D., Influence of water-glass grade and quantity on residual strength of microwave-hardened moulding sands. Part 2, Archives of Foundry Engineering, vol. 11, No 2 (2011) 143-148.
13. Stachowicz M., Granat K., Nowak D., Influence of α-Al2O3 on residual strength of microwave-hardened moulding sands with water-glass, Archives of Foundry Engineering, Special Issue, vol. 11, No 2 (2011) 203-208 (in Polish).
14. Major-Gabryś K., Dobosz St.M., Self-hardened moulding sands with hydrated sodium silicate and liquid ester hardeners, Polish Metallurgy in 2006-2010, Committee of Metallurgy of the Polish Academy of Science, Krakow (2010) 328-335 (in Polish).
15. Major-Gabryś K., Dobosz St.M., The influence of Glassex additive on technological properties and knock-out properties of moulding sands with hydrated sodium silicate and new ester hardeners, Metallurgy and Foundry Engineering, vol.37, No 1 (2011) 33-40.